## Slide 1
CARACTERIZAÇÃO DE FIBRAS CAPILARES
A CIÊNCIA DA MEDIÇÃO POR TRÁS DA INDÚSTRIA DA BELEZA
NATHÁLIA FERRO DE OLIVEIRA
Coordenadora de Avaliação Instrumental & Clínica

## Slide 2
A primeira fórmula de coloração inofensiva
A Fundação da L’Oréal,
Société Française des Teintures
Inoffensives pour Cheveux
1907
Notes: A ciencia e inovaçao sempre estiveram no coraçao do grupo l’Oréal .
A química está em nosso DNA, desde a criaçao de l’Oréal em 1907, com Eugene Schueller, um químico que criou uma primeira tintura inofensiva para cabelos com o nome de L´Oréal.

## Slide 3: O maior investimento da indústria
Chart: 
| 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015
Région 1 | 539 | 582 | 624 | 680 | 748 | 761 | 794
794 M€
Notes: Nós na L´Oréal, pensamos que a ciência é pedra fundamental para a inovação.
Ano após ano o nosso investimento em P&I aumenta, mesmo em momentos de crise.
Por exemplo, em 2015, o grupo fez um investimento de quase 800 milhões de euros em todo o mundo, aproximadamente o dobro de nossos concorrentes.

## Slide 8
Pesquisa GLOCAL
23 Centros de Pesquisa
7
Hubs regionais
Notes: O Centro de P&I brasileiro é um dentre os 7 hubs de pesquisa e inovação criados pela L’Oréal no mundo (ligado ao central, na França), junto com EUA, Japão, Índia, China e África do Sul. Esse tipo de modelo de trabalho faz parte de uma estratégia global da empresa de descentralizar sua area de P&I, buscando atender às necessidades e perfis de consumidores locais.
Dessa maneira, o P&I a AO se tornou uma organizaçao multipolar que é responsável por identificar necessidades dos consumidores local e desenvolver produtos par essas necessidades, mas também que promove a comunicação entre seus centros, criando um rede de Pesquisa e inovaçao

## Slide 9
3870
---- PESQUISADORES
130
---- MOLECULAS EM 40 ANOS
473
---- PATENTES REGISTRADAS
EM 2016
7 mil
----
NOVAS FORMULAS POR ANO
EXCELÊNCIA
científica
Notes: A pesquisa está entre os principais valores da l’Oréal
A força de nossa Pesquisa & Inovação são as mais de 3.800 colaboradores apaixonados pela pesquisa que geram quase 500 patentes anualmente.
Como comparação, esse ambiente gera 30% a mais de patentes que nossos concorrentes do CAC 40, incluindo o mercado de farma.
Nossas equipes também concebem cerca de 7000 novas formulas anualmente, e nesses últimos 40 anos descobriram mais de 40 moléculas.

## Slide 10
Incorporar o ponto de vista do consumidor para aprimorar e avaliar o desempenho percebido do produto
Caracterizar objetivamente as qualidades dos produtos para traduzir a percepção do consumidor em alavancas de design de produtos
Ciência do Consumidor
Ciência Sensorial & Expert
Ciência Instrumental
Ciência Clínica
Garantir a medição objetiva técnica do desempenho do produto para selecionar protótipos e gerar conhecimento
Fornecer evidências de eficácia ativa e desempenho do produto para apoiar lançamentos e comunicação de produtos
AVALIAÇÃO DE DESEMPENHO DE PRODUTO
Notes: Adapt Evaluation plan & process depending on project type
  HIPE for R1 and R5
  Fast & integrated Evaluation for Open Lab projects
  Brief and Pyramid for all projects
  Garantir a confiabilidade
  Calibração das pessoas
  Human social science

## Slide 11
Ciência Instrumental
Garantir a medição objetiva técnica do desempenho do produto para selecionar protótipos e gerar conhecimento
SUPORTE À FORMULAÇÃO
DOSSIERS DE EFICIÊNCIA PARA REIVINDICAÇÕES
DESENVOLVIMENTO DE NOVOS MÉTODOS
GERAÇÃO DE CONHECIMENTO EM PELE E CABELO
AVALIAÇÃO INSTRUMENTAL
Notes: Adapt Evaluation plan & process depending on project type
  HIPE for R1 and R5
  Fast & integrated Evaluation for Open Lab projects
  Brief and Pyramid for all projects
  Garantir a confiabilidade
  Calibração das pessoas
  Human social science

## Slide 12
Eveness
COLOR
SURFACE
STRUCTURE
Spots
Carnation
Pigmentation/Tanning
Redness/Erythema
Vascularisation
Shininess
Sebum
Hydration/Dryness
Pores
Wrinkles
Micro-relief
pH
Sweat
Barrier function
Transparency
(Epi)Dermis structure
Thickness
Water mobility
Firmness/Elasticity
Volume
Micro-circulation
Cells (Size, Renewal)
PPE excellence in measurements / Facial skin attributes
Notes: Ajouter propriétés bioméca (viscoelasticité)

## Slide 13
SURFACE
Shine
Softness
Combing
Smoothness
Lubrificant
Wear resistance
Diameter
Volume
Curl definition
COLOR
STRUCTURE (Shape/Integrity)
Fragility
Damage (Bulk)
Mechanical Resistance
Surface color
Fading
Brushing
Suppleness
Protection
Damage (Surface)
Discipline
Sebum
Density / growth rate
Length
Sweat
Twist definition
Sensitization
Movement
PPE excellence in measurements / Hair attributes
Notes: Transformer méthodes en attributs + compléter par illustrations méthodos

## Slide 14
AVALIAÇÃO INSTRUMENTAL
DESAFIO
VERBALIZAÇÃO DO CONSUMIDOR
VOCABULÁRIO TÉCNICO
Cabelo MACIO
Indentação
método de avaliação
Cabelo HIDRATADO
Conteúdo de água
método de avaliação
método de avaliação
Cabelo LEVE
Massa
Notes: Adapt Evaluation plan & process depending on project type
  HIPE for R1 and R5
  Fast & integrated Evaluation for Open Lab projects
  Brief and Pyramid for all projects
  Garantir a confiabilidade
  Calibração das pessoas
  Human social science

## Slide 15
AVALIAÇÃO INSTRUMENTAL
DESAFIO
VOCABULÁRIO DO CONSUMIDOR
VOCABULÁRIO TÉCNICO
Cabelo MACIO
Indentação
método de avaliação
Cabelo HIDRATADO
Conteúdo de água
método de avaliação
método de avaliação
Cabelo LEVE
Massa
TRADUÇÃO DE PERCEPÇÕES SENSORIAIS EM ATRIBUTOS FÍSICOS OU QUÍMICOS
Notes: Adapt Evaluation plan & process depending on project type
  HIPE for R1 and R5
  Fast & integrated Evaluation for Open Lab projects
  Brief and Pyramid for all projects
  Garantir a confiabilidade
  Calibração das pessoas
  Human social science

## Slide 16
FLEXABRASION APPLIED TO THE EVALUATION OF THE PHOTO DEGRADATION OF HAIR FIBERS
Hair photo damage

## Slide 17
Which are the markers of hair photodamage?

## Slide 18
Brazilian climatological scenario
Annual mean of horizontal global solar radiation
Annual mean of relative humidity
Atlas brasileiro de energia solar / Enio Bueno Pereira; Fernando Ramos Martins; Samuel Luna de Abreu e Ricardo Rüther. – São José dos Campos : INPE, 2006

## Slide 19
Annual mean of horizontal global solar radiation
Annual mean of relative humidity
Brazilian climatological scenarium
L’Oréal BR - Projeto de pesquisa: Estudos meteorotrópicos no Brasil

## Slide 20
Brazilian specificities
High exposure to elevated temperature
High exposure to elevated relative humidity
4th biggest Market for hair products (Euromonitor 2018)
Concerned about solar damage
Need of reliable products to help them in their routines

## Slide 21
Literature review
CHEMICAL CHANGES
STRUCTURAL CHANGES
BEHAVIOR CHANGES
Notes: CUTÍCULAS

## Slide 22
Literature review
CHEMICAL CHANGES
Aminoacids
Lipids
Pigment
cysteine
Tryptophan
Phenylalanine
Histidine
Proline
Valine
18-MEA
Eumelanin
Pheomelanin

## Slide 23
Literature review
STRUCTURAL CHANGES
Cleavage of important bonds
S-S | C-C | C-S
Cracks and cavities on the cuticles surface
Thinning and melting of cuticles
Lift and cracks of the cuticles edges
CMC degradation
Smaller cristaline domains
Higher amount of crosslinks in the matrix
Notes: 36, 37, 8, 27, 38, 7, 6, 5, 39, 40, 9, 41, 42, 10

## Slide 24
Literature review
BEHAVIOR CHANGES
Cuticles more rigid and fragile
Surface more hydroplilic, polar and negative
Easiness of swelling and solubilization
Reduction of mechanical properties
Color fading

## Slide 25
variables
SUBSTRATE
SOURCE
IRRADIANCE
DOSE
ENVIRONMENT
POSITION

## Slide 26
HAIR SUBSTRATE
VARIABLES
Origin
Brazilian
Caucasian
Asian…
Pigmentation
Grey
Blond
Brown…
Sensitization
Natural
Bleached
Transformed...
Our study
Brazilian hair
Brown 4/5
Different sensitization
Natural - NA
Bleached - DE
Colored - CO
Transformed with
formol - AL

## Slide 27
SOURCE OF RADIATION
VARIABLES
Our study
Xenon arc lamp
Ci3000 from Atlas Material Testing Solutions
From: Atlas Materials Testing solutions.
Specific inner and outer filters

## Slide 28
INTENSITY OF RADIATION
Our study
to the window of 300 a 400 nm
VARIABLES
From: ASTM G173-03
Irradiance |  |  | 
Direct | 892,72 | 30,52 | 29,25
Hemispheric (37 ° N) | 993,00 | 46,10 | 21,54
Irradiance |  |  | 
Direct | 892,72 | 30,52 | 29,25
Hemispheric (37 ° N) | 993,00 | 46,10 | 21,54

## Slide 29
DOSE OF RADIATION
VARIABLES
Our study
Time of exposure
Chart: Months of 2015
Manaus 3°06′06″ S | 147.6274 | 211.1619 | 214.6685 | 244.7462 | 153.6327 | 198.8839 | 180.7554 | 110.5066 | 181.8586 | 291.433 | 392.2983 | 382.1067
Fortaleza 3°43′01″ S | 366.141 | 341.5499 | 364.6763 | 299.3459 | 251.9803 | 231.1513 | 194.6077 | 328.5708 | 294.3345 | 307.2965 | 422.6219 | 502.3251
Rio de Janeiro 22°54′10″ S | 710.9871 | 581.7394 | 465.2899 | 441.1873 | 403.2549 | 329.7155 | 351.8861 | 475.3837 | 413.6145 | 540.0943 | 481.3665 | 629.9893
Porto Alegre 30°01′59″ S | 365.2834 | 341.6622 | 363.7284 | 298.6539 | 251.26 | 231.0886 | 194.5324 | 321.2885 | 295.3862 | 307.0112 | 421.8569 | 502.5805
Considering 1,5 h of exposure per day:
~ 1 summer month RJ
~ 1,2 years RJ
Time of exposure
10 h xenon ~ 40 h RJ
to
150 h xenon ~ 600 h RJ

## Slide 30
ENVIRONMENTAL CONDITIONS
VARIABLES
Temperature
Relative humidity
Our study
T = 40 °C
RH = 50 %

## Slide 31
POSITIONING OF THE SAMPLES
VARIABLES
Tresses preparation
Positioning from the lamp
Our study
Flat swatches
Equidistance from the lamp

## Slide 32
Our study
Brazilian hair
Brown 4/5
Different sensitization
Xenon arc lamp
Ci3000 from Atlas Material Testing Solutions
to the window of 300 a 400 nm
10 h to 150 h of exposure
T = 40 °C
RH = 50 %
Flat swatches
Equidistance from the lamp

## Slide 33
  Fibrestress DTM-371 da Textechno – Textile Testing Technology
  Weight with mass of 20 g
  Cyclic movements
  Amplitude: 10 mm
  Frequency: 0,5 Hz
  Abrasion degree: 90°
  Number of fibers analyzed: 50
  Output: Number of cycles before rupture
flexabrasion
Hair breakage -> A consumer perceived sign of damage
Traction
Abrasion
Flexion

## Slide 34
Flexabrasion results
Statistical analysis for t = 0 h
Kruskal-Wallis, with significant level 5 %
Chart: Exposure time (h)
| 0 | 10 | 30 | 60 | 90 | 120 | 150
NA | 438.5 | 426.5 | 397 | 389.5 | 302.5 | 338.5 | 254
DE | 273.5 | 255.5 | 247.5 | 213.5 | 210.5 | 240 | 187
CO | 304.5 | 312.5 | 280.5 | 287.5 | 282.5 | 254.5 | 250.5
AL | 34 | 18.5 | 22 | 17.5 | 26.5 | 34 | 17
Sample | Groups |  | 
AL – 0 h | A |  | 
DE – 0 h |  | B | 
CO – 0 h |  | B | 
NA – 0 h |  |  | C
NA more resistent
DE and CO – no significant differences
AL less resistent

## Slide 35
Natural brazilian hair
Statistical analysis
Mann-Whitney – Comparison to t = 0 h
Chart: Tempo de exposição (h)
| 0 | 10 | 30 | 60 | 90 | 120 | 150
NA | 454.8571 | 429.12 | 417.74 | 379.86 | 303.1957 | 332.14 | 276.76
The higher the exposure time, the lower the number of cycles.
Sample | 10 h | 30 h | 60 h | 90 h | 120 h | 150 h
NA | = | = | ≠ | ≠ | ≠ | ≠
DE | = | = | ≠ | = | = | ≠
CO | = | = | = | = | ≠ | ≠
AL | = | ≠ | ≠ | = | = | ≠

## Slide 36
Bleached and colored brazilian hair
Statistical analysis
Mann-Whitney – Comparison to t = 0 h
The higher the exposure time, the lower the number of cycles.
Lower angular coeficiente compared to NA: Lower impact of the radiation kinetics.
Sample | 10 h | 30 h | 60 h | 90 h | 120 h | 150 h
NA | = | = | ≠ | ≠ | ≠ | ≠
DE | = | = | ≠ | = | = | ≠
CO | = | = | = | = | ≠ | ≠
AL | = | ≠ | ≠ | = | = | ≠
Chart: Tempo de exposição (h)
| 0 | 10 | 30 | 60 | 90 | 120 | 150
DE | 267.06 | 243.2 | 238.44 | 215.46 | 223.04 | 215.46 | 184.78
CO | 317.96 | 285.44 | 277.92 | 265.94 | 264.8 | 252.04 | 240.02

## Slide 37
transformed brazilian hair
Statistical analysis
Mann-Whitney – Comparison to t = 0 h
Number of cycles do not depend on the exposure time.
Sample | 10 h | 30 h | 60 h | 90 h | 120 h | 150 h
NA | = | = | ≠ | ≠ | ≠ | ≠
DE | = | = | ≠ | = | = | ≠
CO | = | = | = | = | ≠ | ≠
AL | = | ≠ | ≠ | = | = | ≠
Chart: Tempo de exposição (h)
| 0 | 10 | 30 | 60 | 90 | 120 | 150
AL | 34.0208 | 29.68 | 28.08 | 25.3878 | 30.02 | 33 | 24.14

## Slide 38
conclusion
  Flexabrasion is Indicated to evaluate the damaging effects of solar radiation into hair fibers
  Moreover it is a potential methodology to evaluate the efficacy of hair photo protection products

## Slide 39
References
COSMETIC & TOILETRIES. Hair Care: From Physiology to Formulation. Carol Stream, IL: Allured Business Media.
ROBBINS, C. Chemical and Physical Behavior of Human Hair. 5. ed. New York: Springer-Verlag, 2012.
RICHENA, M.; REZENDE, C. A. Effect of photodamage on the outermost cuticle layer of human hair. Journal of Photochemistry & Photobiology, B: Biology, v. 153, p. 296–304, 2015.
GAO, T.; BEDELL, A. Ultraviolet damage on natural gray hair and its photoprotection. Journal of Cosmetic Science, v. 52, p. 103-118, 2001.
NOGUEIRA, A. C. S.; Joekes, I. Hair color changes and protein damage caused by ultraviolet radiation. Journal of Photochemistry and Photobiology B: Biology, v. 74, p. 109–117, 2004.
NOGUEIRA, A. C. S. Foto-degradação do cabelo: influência da pigmentação da fibra. 2008. Tese (Doutorado no Instituto de Química)- Universidade Estadual de Campinas, Campinas, SP, Brasil, 2008.
RICHENA, M.; REZENDE, C. A. Morphological degradation of human hair cuticle due to simulated sunlight irradiation and washing. Journal of Photochemistry & Photobiology, B: Biology, v. 161, p. 430–440, 2016.
RUETSCH, S. B.; KAMATH, Y.; WEIGMANN, H. D. Photodegradation of human hair: An SEM study. Journal of Cometics Science, v. 51, p. 103-125, 2000.
HOTING, E.; ZIMMERMANN, M.; HILTERHAUS-BONG, S. Photochemical alterations in human hair: I. Artificial irradiation and investigations of hair proteins. J. Soc. Cosmet. Chem, v. 46, p. 85-99, 1995.
JEON, S. Y.; PI, L. Q.; LEE, W. S. Comparison of hair shaft damage after UVA and UVB irradiation. J. Cosmet. Sci. v. 59, p. 151-156, 2008.
PANDE. C. M.; JACHOWICZ, J. Hair photodamage Measurement and prevention. J. Soc. Cosmet. Chem. V. 44, p. 109-122, 1993.
FERNÁNDEZ, E. et al. Photodamage determination of human hair. Journal of Photochemistry and Photobiology B: Biology, v. 106, p. 101–106, 2012.
CHANDRASHEKARA, M. N.; RANGANATHAIAH, C. Chemical and photochemical degradation of human hair: A free-volume microprobe study. Journal of Photochemistry and Photobiology B: Biology, v. 101, p. 286–294, 2010.
RATNAPANDIAN, S.; WARNER, S. B.; KAMATH, Y. K. Photodegradation of human hair. J. Cosmet. Sci. v. 49, p. 309-320, 1998.